# Certificate of Analysis

Name of Product : Chitosan 60 FG – Chitosan Oligosaccharide Lactate                                      Lenzites Betulina Mushroom Source

CAS No. : 148411-57-8

Batch / Lot No. : PRM/CHT-60FG/01/01-2026 Date of Mfg. : January 2026

Date of Exp. : December 2028

Manufactured by : Promecens Entosystems Private Limited

| Sr. No. | Test / Parameter | Specification | Result |
| --- | --- | --- | --- |
| 1 | Appearance | Light brown / cream / off- white, free-flowing powder | Cream-colored, free-flowing powder |
| 2 | Degree of Deacetylation | ≥ 95% | 98.67 % |
|  | Purity | 98.0 - 99.5 % | 99.13% |
| 3 | Solubility (1 g in 100 mL DI water; magnetically stirred 1-2 h at RT; do not heat) | Completely soluble in water | Passes |
|  | Zeta Potential | +55 - 65 mV | +59.77 mV |
| 4 | pH (1% solution in DI water, 25-30°C) | 2.0 - 5.5 | 4.48 |
| 5 | Viscosity (1% aq. solution, 30°C) | 0.10 - 100 cSt | 6.59 cSt |
| 6 | Heavy metals (as Pb) | NMT 10 ppm | NIL |
| 7 | Soluble fraction in DM water | 8.0 - 10.0 % | 9.69 % |
| 8 | Insoluble in water | NMT 1.0 % | 0.01 % |

Remarks:

The product meets all required quality specifications and has passed comprehensive quality testing for solubility, pH, viscosity, and appearance.

Authorized Signatory:

Promecens Entosystems Private Limited