Certificate of Analysis

Promecens Chitosan Oligosaccharide

Product Name: Chitosan Oligosaccharide - Fungal

Batch No.: COS/01/2026

CAS No.: 148411-57-8

Molecular Weight (Avg.): < 3 kDa (Customizable)

Date of Manufacture: January 2026

Expiry Date: December 2027

Manufacturer: Promecens Entosystems Private Limited

Test Results

| Parameter | Specification | Result |
| --- | --- | --- |
| Appearance | Off-white/light brown powder or flakes | Off-white or light brown powder |
| Purity Degree of Deacetylation | 95% - 100% 90% - 98% | 99.55% 98.14% |
| Viscosity (cS) | 1 – 20 cS | 1.8 cS |
| Water Solubility (1g/100ml, RT) | Soluble (with stirring) | Passes |
| pH (1% solution in distilled water) | 2.0 - 5.5 | 3.25 |
| Dissolved Soluble Fraction in DM Water (Dilution Factor 1/10) | 8% - 10% (Measured Concentration * 10) | 9.90% * 10 = 99% |
| Insoluble Matter in Water | Max 1% | 0.10% |

Remarks

The product meets all required quality specifications and has passed comprehensive quality testing for solubility, viscosity, and purity.

Issued on behalf of Promecens Entosystems Pvt. Ltd.