## Slide 1
Chitosan IG for Barentz HI&I — Executive Overview
What it is: Chitosan Oligosaccharide Hydrochloride (Chitosan IG), a highly water‑soluble, low‑MW, cationic biopolymer with ~70 mV zeta potential derived from mushroom or insect chitin.
Why Barentz: Delivers multi‑category performance roles including soil suspension, anti‑redeposition, rinse clarity, film formation, and streak/spot control coupled with a strong sustainability profile.
Scope of Opportunity: Addresses 7 HI&I categories including Laundry, Dishwash, Floor Care, Hard Surface, Industrial Cleaning, Textile/Carpet, and Vehicle Care with optimized cost-in-use formulations.
Commercial Parameters
Selling Price (FOB, Freight Not Included): 1–499 kg: $105.30/kg | 500–999 kg: $97.20/kg | ≥1,000 kg: $89.10/kg
Application Rate: 0.01-0.10% w/w

## Slide 2
Laundry — How Chitosan IG Fits
Incumbent Set: Anionic/nonionic surfactants (LAS/SLES, AE), acrylics (PAA, CMC), chelants, and enzymes.
IG Roles: Anti‑redeposition booster, soil release aid, rinse clarity/flocculation, and fabric conditioning.
Application Rates: 0.02–0.08% w/w for liquids; 0.05–0.10% w/w for powders.
Formulation Tips: Add in cool‑down, maintain pH 5–8.5, and pair with APGs.
Cautions & Limitations
Avoid: Hypochlorite and strong oxidants.
Manage Anionic Loads: High anionic loads can suppress the cationic benefit—stage addition carefully.

## Slide 3
Laundry — Cost Comparison
Selling Price (FOB, Freight Not Included): $89.10/kg (≥1,000 kg) | $97.20/kg (500–999 kg) | $105.30/kg (1–499 kg)
Incumbent Benchmarks (per kg):
SLES 70%: $1.5–$2.3 | Acrylic Dispersant: $2.0–$3.0 | Solvent (Glycol Ether): $1.6–$2.2
EDTA: $1.7–$2.5 | Enzymes: $20–$40
IG Addition Cost (per 1,000 kg batch): 0.02% (0.2 kg) = $17.82 | 0.03% (0.3 kg) = $26.73 | 0.05% (0.5 kg) = $44.55
Cost Scenarios (Net impact vs. current ingredient set per 1,000 kg batch):
Minimal (IG 0.02%): +$13.6 to +$14.6
Balanced (IG 0.03%): +$14.9 to +$16.9
Aggressive (IG 0.02%): -$6.0 to +$2.0
Recommendation
Start at 0.02–0.03% targeting partial acrylic dispersant and modest surfactant/solvent reductions. Optimize formulation after validating wash performance.

## Slide 4
Dishwash — How Chitosan IG Fits
Incumbent Set: Manual: SLES/AES + APG, solvents, salts/viscosity builders, acrylic dispersants. Auto: Enzymes, anti-spot polymers, rinse aids.
IG Roles: Soil suspension and anti‑redeposition, streak and film control via cationic microfilm, foam quality modulation with APG, and rinse clarity improvement; adjunct to anti‑spot in auto.
Application Rates: Manual: 0.01% – 0.05% w/w | Auto: 0.02% – 0.06% w/w.
Formulation Tips & Cautions
Tips: Pair with APG/nonionics for stability; validate glass streak and spot metrics; maintain pH 5–8.
Cautions: Limit exposure to chlorine bleach; manage anionic:cationic ratio to avoid viscosity shocks or phase separation.

## Slide 5
Dishwash — Cost Comparison
Selling Price (FOB, Freight Not Included): $89.10/kg (≥1,000 kg) | $97.20/kg (500–999 kg) | $105.30/kg (1–499 kg)
Incumbent Benchmarks (per kg):
SLES: $1.5–$2.3 | APG: $2.0–$3.0 | Acrylic Dispersant: $2.0–$3.0
Solvent: $1.6–$2.2 | Fragrance: $8–$15
IG Addition Cost (per 1,000 kg batch): 0.015% (0.15 kg) = $13.37 | 0.02% (0.2 kg) = $17.82
Cost Scenarios — Net impact vs. current ingredient set per 1,000 kg batch:
Minimal (IG 0.015%): +$9.5 to +$10.5
Balanced (IG 0.02%): +$8.6 to +$11.6
Aggressive (IG 0.02%): -$0.4 to +$1.6
Recommendation
Position in premium no-streak/eco SKUs; tune acrylic and surfactant reductions to approach neutral economics.

## Slide 6
Floor Care — How Chitosan IG Fits
Incumbent Set: Acrylic/metal-crosslinked polymer emulsions, wax emulsions, plasticizers, leveling aids, and defoamers.
IG Roles: Functions as a co-binder and film modifier. It improves scuff resistance, early hardness, recoat adhesion, and dirt pick-up resistance, with the potential to reduce zinc crosslinker requirements.
Application Rates: 0.05% - 0.20% on total formula. Should be added post-neutralization to ensure stability.
Formulation Tips: Screen with target acrylics for minimum film forming temperature and leveling. Check gloss build and black-heel mark resistance. Optimal performance at pH 7-9.
Cautions & Considerations
Formulation Watch-outs: Avoid using hypochlorite maintenance cleaners over fresh films. Always verify clarity and compatibility in high-solids systems.

## Slide 7
Floor Care — Cost Comparison
Selling Price (FOB, Freight Not Included): $89.10/kg (≥1,000 kg) | $97.20/kg (500–999 kg) | $105.30/kg (1–499 kg)
Incumbent Benchmarks (per kg):
Acrylic Emulsion Solids: $1.8–$2.8 | Wax Emulsion: $1.8–$2.5
Zinc Crosslinker: $2.0–$3.0
IG Addition Cost (per 1,000 kg batch): 0.05% (0.5 kg) = $44.55 | 0.08% (0.8 kg) = $71.28 | 0.10% (1.0 kg) = $89.10
Cost Scenarios (Net impact vs. current ingredient set per 1,000 kg batch):
Minimal (IG 0.05%): +$16.6 to +$26.6
Balanced (IG 0.08%): +$16.5 to +$22.5
Aggressive (IG 0.10%): +$3.0 to +$19.0
Recommendation
Market as a premium finish modifier to defend price via durability claims rather than raw cost only.

## Slide 8
Hard Surface Cleaning — How Chitosan IG Fits
Incumbent Set: Anionic/nonionic surfactants, glycol-ether solvents, organic acids, acrylic dispersants, silicates.
IG Roles: Anti-redeposition and soil suspension, streak and film control, rinse water clarification, synergy with organic acids, and improved particulate capture in mops and pads.
Application Rates: 0.02% – 0.08% w/w.
Formulation Tips: Combine with APGs for eco-claims, validate gloss and streak metrics, pH 4.0–8.5 preferred.
Cautions & Limitations
Limit oxidizers; manage high anionic loads carefully by staging or split-adding during formulation to avoid precipitation.

## Slide 9
Hard Surface Cleaning — Cost Comparison
Selling Price (FOB, Freight Not Included): $89.10/kg (≥1,000 kg) | $97.20/kg (500–999 kg) | $105.30/kg (1–499 kg)
Incumbent Benchmarks (per kg):
SLES: $1.5–$2.3 | Acrylic Dispersant: $2.0–$3.0 | Solvent: $1.6–$2.2
IG Addition Cost (per 1,000 kg batch): 0.02% (0.2 kg) = $17.82 | 0.03% (0.3 kg) = $26.73
Cost Scenarios (Net impact vs. current ingredient set per 1,000 kg batch):
Minimal (IG 0.02%): +$10.6 to +$12.6
Balanced (IG 0.03%): +$12.9 to +$13.9
Aggressive (IG 0.02%): -$4.4 to +$0.6
Recommendation
Best fit in premium streak-free and bathroom SKUs. Performance improvements can justify near-neutral economics.

## Slide 10
Industrial Cleaning — How Chitosan IG Fits
Incumbent Set: Alkalies/solvents, surfactants, chelants, silicates, corrosion inhibitors.
Chitosan IG Roles: Anti-redeposition under high soil load, fines/metal particulate capture, clarifies spent baths, reduces downstream filter load, and provides light flash-rust inhibition via film formation.
Application Rates: 0.02% – 0.10% depending on bath turnover.
Formulation Tips: Dose inline or in concentrate to maintain ppm levels; validate performance via DCO or soil load ramp tests.
Cautions & Limitations
Avoid These Conditions: Very high pH and strong oxidants reduce the benefit. Always check corrosion inhibitor compatibility.

## Slide 11
Industrial Cleaning — Cost Comparison
Selling Price (FOB, Freight Not Included): $89.10/kg (≥1,000 kg) | $97.20/kg (500–999 kg) | $105.30/kg (1–499 kg)
Incumbent Benchmarks (per kg):
Surfactant Blend: $1.8–$2.6 | Silicate: $0.9–$1.3 | Solvent (Glycol Ether): $1.6–$2.2
EDTA: $1.7–$2.5
IG Addition Cost (per 1,000 kg batch): 0.03% (0.3 kg) = $26.73 | 0.04% (0.4 kg) = $35.64 | 0.05% (0.5 kg) = $44.55
Cost Scenarios (Net impact vs. current ingredient set per 1,000 kg batch):
Minimal (IG 0.03%): +$11.9 to +$15.9
Balanced (IG 0.04%): +$19.2 to +$22.2
Aggressive (IG 0.03% + OPEX): -$2.1 to +$0.9
Recommendation
Sell on total cost of operations (bath life, filter media, waste fees), not raw material alone. Position for overall operational savings.

## Slide 12
Textile/Carpet/Upholstery — How Chitosan IG Fits
Incumbent Set: Surfactants, solvents, acrylic/CMC/PVP anti-redeposition agents, enzymes, defoamers, and odor absorbers.
Chitosan IG Roles: Forms a fiber-affinitive cationic microfilm to prevent redeposition, improves particulate lift in extraction cleaning, reduces dye bleed/transfer risks, and provides an adjunct soft-hand feel.
Recommended Application Rates: 0.02–0.05% w/w in presprays and extractants; 0.05–0.10% w/w in rinse aids and fabric refreshers.
Formulation Tips: Verify colorfastness on target fabrics, align compatibility with defoamer levels, and evaluate resoil metrics post-clean to confirm benefits.
Cautions & Limitations
Formulation Warnings: Avoid strong oxidizers which can degrade the polymer. Carefully manage the anionic surfactant load to prevent coacervate haze formation.

## Slide 13
Textile/Carpet/Upholstery — Cost Comparison
Selling Price (FOB, Freight Not Included): $89.10/kg (≥1,000 kg) | $97.20/kg (500–999 kg) | $105.30/kg (1–499 kg)
Incumbent Benchmarks (per kg):
Anti-Redeposition Polymer: $2.0–$3.0 | Surfactant Blend: $1.8–$2.6
Solvent: $1.6–$2.2 | Enzymes: $20–$40
IG Addition Cost (per 1,000 kg batch): 0.02% (0.2 kg) = $17.82 | 0.03% (0.3 kg) = $26.73
Cost Scenarios (Net impact vs. current ingredient set per 1,000 kg batch):
Minimal (IG 0.02%): +$14.6 to +$15.6
Balanced (IG 0.03%): +$14.9 to +$17.9
Aggressive (IG 0.02%): -$3.4 to +$0.6
Recommendation
Target professional carpet care where lower re-soiling callbacks and fewer re-cleans justify near-neutral raw material costs.

## Slide 14
Vehicle Care — How Chitosan IG Fits
Incumbent Set: SLES/AES + betaines/APG, hydrophobic polymers/waxes, sequestrants, builders.
IG Roles: Enhances soil suspension in high‑soil truck/car washes; improves rinse clarity; acts as a cationic film former for sheeting and anti‑spotting; significantly reduces tunnel carryover soils.
Application Rates: 0.01% – 0.03% w/w in shampoos/foams; 0.02% – 0.05% w/w in presoaks/bug removers.
Formulation Tips: Balance anionic/cationic ratio to maintain foam stability; physically check glass for spotting; best paired with APG or betaine blends for maximum compatibility.
Cautions & Limitations: Very high anionic loads can suppress the cationic performance benefits. Strictly avoid interactions with strong oxidants.

## Slide 15
Vehicle Care — Cost Comparison
Selling Price (FOB, Freight Not Included): $89.10/kg (≥1,000 kg) | $97.20/kg (500–999 kg) | $105.30/kg (1–499 kg)
Incumbent Benchmarks (per kg):
SLES 70%: $1.5–$2.3 | Betaine: $1.8–$2.6 | APG: $2.0–$3.0
Acrylic Dispersant: $2.0–$3.0 | Wax Polymer: $2.0–$4.0
IG Addition Cost (per 1,000 kg batch): 0.01% (0.1 kg) = $8.91 | 0.02% (0.2 kg) = $17.82 | 0.03% (0.3 kg) = $26.73
Cost Scenarios (Net impact vs. current ingredient set per 1,000 kg batch):
Minimal (IG 0.01%): +$7.3 to +$8.3
Balanced (IG 0.02%): +$7.6 to +$10.6
Aggressive (IG 0.02%): +$0.6 to +$3.6
Recommendation
Use in premium tunnels/foams and rinses to defend price via reduced spotting/soiling and faster dry.
John Hott | john@chitosanglobal.com | (423) 440-9795 | chitosanglobal.com